| GNL-5013xx (Φ5mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter Unit DC Forward Current 30 mA Reverse Voltage 5 V Reverse Current (Vr-5V) 10 µA Peak Forward Current ,tw ,=1 msec Duty ,=1/20 150 mA Operation Temperature -40 +80 ℃ Storage Temperature -40 +100 ℃ Solder Dip (3 seconds,1.6mm from body ) Temperature 260 ±5 ℃ |  |
| --- | --- |
| Part Number EMITTED COLOR Lens Color Peak Wavelength (nm) Vf (v) Typ. IV (If=20mA) mcd View Angle 2θ1/2 Min. Typ. GNL-5013SRD GaAlAs Super Red Red Diffused 660 1.9 50 100 60° GNL-5013SRT GaAlAs Super Red Red Transparent 660 1.9 250 400 18° GNL-5013SRC GaAlAs Super Red Water Clear 660 1.9 250 400 18° GNL-5013LRC GaAlAs Super Red Water Clear 660 1.9 400 500 18° GNL-5013LRD GaAlAs Super Red Red Diffused 660 1.9 100 150 60° GNL-5013URC GaAlAs Super Red Water Clear 660 1.9 600 800 18° GNL-5013UEC AlGaInP Super Orange Red Water Clear 625 2.0 1200 1500 18° GNL-5013HRC AlGaInP Super Orange Red Water Clear 640 2.0 500 1000 18° GNL-5013HRD AlGaInP Super Orange Red Red Diffused 640 2.0 250 500 60° GNL-5013GC GaP Green Water Clear 565 2.0 40 50 18° GNL-5013UGC AlGaInP Yellow Green Water Clear 572 2.0 600 800 18° GNL-5013UGD AlGaInP Yellow Green Green Diffused 572 2.0 150 200 60° GNL-5013YC GaAsP Yellow Water Clear 588 2.0 40 50 18° GNL-5013UYC AlGaInP Super Yellow Water Clear 590 2.0 1200 1500 18° GNL-5013BC InGaN Super Blue Water Clear 470 3.5 1000 1500 18° GNL-5013UBC InGaN Ultra Super Blue Water Clear 470 3.5 1500 2000 18° GNL-5013UBW InGaN Ultra Super Blue Milk Diffused 470 3.5 800 1500 60° GNL-5013BGC InGaN Super Bluish Green Water Clear 505 3.5 4000 5000 18° GNL-5013PGC InGaN Super Pure Green Water Clear 525 3.5 5000 7000 18° GNL-5013VC InGaN Super Violet Water Clear 395 3.5 50 100 18° GNL-5013UVC InGaN Ultra Violet Water Clear 270 6.0 2MW 3MW 25° GNL-5013UEC-1 AlGaInP Super Orange Red Water Clear 625 2.0 1000 1200 18° GNL-5013UYC-1 AlGaInP Super Yellow Water Clear 590 2.0 1000 1200 18° GNL-5013PGC-1 InGaN Super Pure Green Water Clear 525 3.5 4000 5000 18° |

# Text boxes

G-NOR ELECTRONICS CO.,LTD.