| GNL-0805xx (0805 SMD TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter Unit DC Forward Current 30 mA Reverse Voltage 5 V Reverse Current (Vr-5V) 10 µA Peak Forward Current ,tw ,=1 msec Duty ,=1/20 150 mA Operation Temperature -40 +80 ℃ Storage Temperature -40 +100 ℃ Solder Dip Temperature (5 seconds,1.6mm from body ) 300 ±5 ℃ |  |
| --- | --- |
| Features: Compatible with automatic placement equipment Compatible with reflow solder process Applications: Automotive and Telecommunication General use for indicators |
| Part Number EMITTED COLOR Lens Color Peak Wavelength (nm) Vf (v) Typ. IV (If=20mA) mcd View Angle 2θ1/2 Min. Typ. GNL-0805GC GaP Green Water Clear 567 2.0 7 12 120° GNL-0805EC GaP Orange Red Water Clear 635 2.0 10 18 120° GNL-0805YC GaAsP Yellow Water Clear 588 2.0 10 18 120° GNL-0805SRC GaAlAs Red Water Clear 660 2.0 9 15 120° GNL-0805UEC AlGaInP Super Red Water Clear 625 2.1 30 40 120° GNL-0805HRC AlGaInP Super Red Water Clear 640 2.1 30 40 120° GNL-0805UEC-TL AlGaInP Super Red Water Clear 625 2.1 120 200 120° GNL-0805UYC AlGaInP Super Yellow Water Clear 587 2.1 30 40 120° GNL-0805UYC-TL AlGaInP Super Yellow Water Clear 592 2.1 100 150 120° GNL-0805PGC InGaN Super Pure Green Water Clear 525 3.4 200 300 120° GNL-0805PGC-TL InGaN Super Pure Green Water Clear 525 3.4 400 600 120° GNL-0805UBC InGaN Super Blue Water Clear 470 3.2 95 150 120° GNL-0805WC InGaN Super White Water Clear 3.2 200 300 120° |

# Text boxes

G-NOR ELECTRONICS CO.,LTD.